## Slide 1: Coking plant – Coal yard
Stacker/re-claimer
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Bearings | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease Li EP 2 |  | PETRONAS Grease LiX Syn 2/220
Gearbox / Reducer | AGMA 4-7 EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Open Gears | AGMA 251.01 FZG US Steel | Pumpability and sprayability Adhesive characteristics Extreme pressure Low consumption | - | PETRONAS Grease LiCa TMG | -
Cables | OIPEEC | Core penetration Adhesive characteristics Elasticity Rust and corrosion protection | PETRONAS Grease LiCa GEP 2.5 | - | -
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Chains | ISO VG 220 Cincinnati Machine Spec | Tackiness Rust and corrosion protection Lubricity | PETRONAS Slideway | - | -

## Slide 2: Coking plant
Conveyor
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Gearbox / Reducer | AGMA 4-7 EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Bearings | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease Li EP 2 |  | PETRONAS Grease LiX Syn 2/220
Coupling | NLGI 2 EP AGMA CG 1 and 2 | Low oil bleed Oxidation stability Resistance to centrifugal force | PETRONAS Grease Li 2 | PETRONAS Grease PE HS | -
Idler roller bearing |  |  | Filled for life - special low viscosity grease (contact OEM for initial fill) |  | 

## Slide 3: Coking plant
Jaw Crusher (Primary Crusher)
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Plain Bearings / Roller bearings | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Gearbox / Reducer | AGMA 4-7 EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Hydraulics | Premium VI High VI | Water Separability Wet and Dry Filterability Multi metal compatibility Rust and corrosion protection | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF

## Slide 4: Coking plant
Cone Crusher (Secondary Crusher)
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Plain Bearings | AGMA 4EP | High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Spider bush bearing (Grease) | NLGI 2 | High load capability High and low temperature handling Mechanical stability | PETRONAS Grease LiX MEP | PETRONAS Grease LiCa MG HL | PETRONAS Grease LiCa MG XHL
Spider bush bearing (oil) | AGMA 4EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Gearbox / Reducer | AGMA 4EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Hydraulics | Premium VI High VI | Water Separability Wet and Dry Filterability Multi metal compatibility Rust and corrosion protection | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF

## Slide 5: Coking plant
Gyratory Crusher (Secondary Crusher)
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Plain Bearings | AGMA 4EP | High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Spider bush bearing (Grease) | NLGI 2 | High load capability High and low temperature handling Mechanical stability | PETRONAS Grease LiX MEP | PETRONAS Grease LiCa MG HL | PETRONAS Grease LiCa MG XHL
Spider bush bearing (oil) | AGMA 4EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Gearbox / Reducer | AGMA 4EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Hydraulics | Premium VI High VI | Water Separability Wet and Dry Filterability Multi metal compatibility Rust and corrosion protection | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF

## Slide 6: Coking plant
Impact Crusher (Secondary Crusher)
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Plain Bearings | AGMA 4EP | High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Spider bush bearing (Grease) | NLGI 2 | High load capability High and low temperature handling Mechanical stability | PETRONAS Grease LiX MEP | PETRONAS Grease LiCa MG HL | PETRONAS Grease LiCa MG XHL
Spider bush bearing (oil) | AGMA 4EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Gearbox / Reducer | AGMA 4EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Hydraulics | Premium VI High VI | Water Separability Wet and Dry Filterability Multi metal compatibility Rust and corrosion protection | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF

## Slide 7: Coking plant - Screening
Breaker Screen
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Greased Bearings | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/220
Hydraulics | Premium VI High VI | Water Separability Wet and Dry Filterability Multi metal compatibility Rust and corrosion protection | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF

## Slide 8: Coking plant
Mixer
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Gearbox / Reducer | AGMA 4EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO

## Slide 9: Coking plant
Larry / Charge car
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Contact Bearing | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | Extreme High temperature Dust | PETRONAS Grease Li EP 2 | PETRONAS Grease CaSX | PETRONAS Grease LiX Syn 2/220
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -

## Slide 10: Coking plant
Coke oven
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Fire Resistance Hydraulic | Fire resistant Premium VI High VI | High temperature Dust | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
Contact Bearing | Li complex / Ca Sulfonate complex NLGI 2 Dust handling polymer thickener | Extreme High temperature Dust | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Grease points (Charge & pusher car) | Li complex / Ca Sulfonate complex NLGI 2 Dust handling polymer thickener | High temperature Dust High load | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Gearbox / Reducer | ISO VG 320 or 460 FZG Temperature range | High temperature Dust | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAG**
Compressors | DIN 51506 VDL | High temperature | PETRONAS Compressor A M2 | PETRONAS Compressor A M4 | PETRONAS Compressor A Syn
Butterfly / actuator valve | NLGI 2 | High temperature Dust Solid lubricants | PETRONAS Grease LiCa GEP 2.5 | PETRONAS Grease LiX MEP | PETRONAS Grease LiCa MG HL
Electric motors | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
**special precautions needed

## Slide 11: Coking plant
Quench Car
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Journal Bearings (oil) | ISO VG | High load High temperature Oxidation stability | PETRONAS Circula | - | PETRONAS Circula Syn
Journal Bearings (Grease) | NLGI 2 | High load High temperature Oxidation stability | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Diesel engine (Two stroke) | 20W-40 Rail type | Cold starting Long idling periods Soot handling | PETRONAS Genrail V | - | PETRONAS Genrail Syn VI
Cooling System | Coolant Fluid | Long periods of work High temperature | PETRONAS Paraflu 11 | PETRONAS Paraflu Up Ready | -
Gearbox / Reducer | ISO VG 320 or 460 FZG Temperature range | High temperature Dust | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO/ PAG**
Fire Resistance Hydraulic | Fire resistant Premium VI High VI | High temperature Dust | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
**special precautions needed

## Slide 12: Coking plant
Quenching tower (in quench car)
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Bearings (Oil) | ISO VG 68 | Demulsibity Low foaming tendencies Antiwear properties | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF
Bearings (Grease) | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease Li EP 2 |  | PETRONAS Grease LiX Syn 2/220
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -

## Slide 13: Coking plant - Screening
Screening plant
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Greased Bearings | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Electric motors | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -

## Slide 14: Iron Production
Blast Furnace
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Hydraulics | Fire resistant Premium VI High VI | High temperature Dust | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
Contact Bearings | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | Extreme High temperature Dust | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Turbine (Tuyeres) | Siemens | Low foaming Rapid air release Water separability Thermal stability | PETRONAS Jenteram | Petronas Gear 6800 | PETRONAS Jenteram Syn
Compressors (Tuyeres) | DIN 51506 VDL | Oxidation stability Reduced deposits Long drain intervals | PETRONAS Compressor A M2 | PETRONAS Compressor A M4 | PETRONAS Compressor A Syn
Blower (Fan) | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease PU |  | PETRONAS Grease LiX Syn 2/100
Blower (Compressor) | DIN 51506 VDL | Oxidation stability Reduced deposits Long drain intervals | PETRONAS Compressor A M2 | PETRONAS Compressor A M4 | PETRONAS Compressor A Syn
Actuator valves | NLGI 2 Solid lubricants | High temperature Dust | PETRONAS Grease LiCa GEP 2.5 | PETRONAS Grease LiX MEP | PETRONAS Grease LiCa MG HL
Tap hole drill | Fire resistant Premium VI High VI | High temperature Dust | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
Mud Gun | Fire resistant Premium VI High VI | High temperature Dust | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -

## Slide 15: Hot Metal Pre-treatment
Torpedo Cars / ladle
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Contact Bearing | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | High temperature Fire sparks Dust | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Rail bearing support | NLGI 2 | High temperature Fire sparks Dust | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Gearbox / Reducer | AGMA 4-7 EP | Extreme high temperature Dust | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAG**
Grease points (Rails) | NLGI 2 | High temperature Fire sparks Dust | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Diesel engine (Two stroke) | 20W-40 Rail type | Cold starting Long idling periods Soot handling | PETRONAS Genrail V | - | PETRONAS Genrail Syn VI
Cooling System | Coolant Fluid | Long periods of work High temperature | PETRONAS Paraflu 11 | PETRONAS Paraflu Up Ready | -
Journal bearings (oil) | ISO VG 150 | High load High temperature Oxidation stability | PETRONAS Circula | - | PETRONAS Circula Syn
**special precautions needed

## Slide 16: Primary Steelmaking
Converter / Basic Oxygen Furnace / Re-melter
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Contact bearing | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | Solid lubricants High temperature capability | - | PETRONAS Grease CaSX | 
Gearbox / Reducer | ISO VG 320 or 460 FZG Temperature range | Extreme high temperature Dust | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAG**
Movable seal | NLGI 2 | Solid lubricants High temperature capability | - | - | PETRONAS Ceramic paste
**special precautions needed

## Slide 17: Primary Steelmaking
Electric arc furnace (EAF)
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Compressor (Air brake) | DIN 51506 VDL | High temperature Fire sparks | PETRONAS Compressor A M2 | PETRONAS Compressor A M4 | PETRONAS Compressor A Syn
Hydraulic System | Fire resistant Premium VI High VI | High temperature Fire sparks | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
Support Bearings | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | Extreme high temperature Dust | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Open Gears and Plates | AGMA 251.01 FZG US Steel | Extreme high temperature Dust | - | PETRONAS Grease LiCa TMG | -

## Slide 18: Secondary Steelmaking
Ladle
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Compressor (Air brake) | DIN 51506 VDL | High temperature Fire sparks | PETRONAS Compressor A M2 | PETRONAS Compressor A M4 | PETRONAS Compressor A Syn
Hydraulic System | Fire resistant Premium VI High VI | High temperature Fire sparks | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
Support Bearings | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | Extreme high temperature Dust | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/460
Open Gears and Plates | AGMA 251.01 FZG US Steel | Extreme high temperature Dust | - | PETRONAS Grease LiCa TMG | -

## Slide 19: Continuous Casting
Continuous Casting Machine
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Special Contact Bearing | Li complex / Ca Sulfonate complex NLGI 2 | Extreme High temperature Water Extreme load carrying | - |  | PETRONAS Grease LiX Syn 2/460
Slewing bearing | NLGI 2 EP | High temperature Fire sparks High load carrying | - | - | PETRONAS Grease LiCa XHL
Gearbox / Reducer | AGMA 4-7 EP | High temperature Dust | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO/ PAG*
Hydraulic System | Fire resistant Premium VI High VI | High temperature Water | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
**special precautions needed

## Slide 20: Hot Rolling
Hot Rolling
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Bearings (Furnace, Roller Table, Finishing Roller) | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | High temperature Load carrying | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/220
Morgan Bearing | ISO VG 100 – 460 FZG | Rapid demulsibility Oxidation Stability | PETRONAS Mill | PETRONAS Mill NT Series Petronas Gear 6800 | -
Gearbox / Reducer (Rollers, Roller Tables, Finishing Rollers, Winders | ISO VG 320 or 460 FZG Temperature range | Extreme high temperature Dust | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAO/ PAG**
Hydraulic System (Rolling Gearbox / Reducer, Roller Table) | Fire resistant Premium VI High VI | Fire Resistance | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
Electric motors | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Open Gears (Grease) - Winder | AGMA 251.01 FZG US Steel | High temperature Dust | - | PETRONAS Grease LiCa TMG | -
Cooling bed support bearings | NLGI 2 | High temperature High load Water tolerance | - | PETRONAS Grease CaSX | -
**special precautions needed

## Slide 21: Power generation
Gas turbine or Gas engines
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Gas turbine (with/without associated geardrives) | Siemens, Alstom, GE, Toshiba, Mitsubishi | Low foaming Rapid air release Water separability Thermal stability | - | Petronas Jenteram G | -
Gas turbine (without associated geardrives) | Siemens, Alstom, GE, Toshiba, Mitsubishi | Low foaming Rapid air release Water separability Thermal stability | - | Petronas Jenteram G | -
Gas engine | Wartsilla GE | Low ash TBN retention Soot control Low deposits | PETRONAS GEO BLG or Petronas NG | - | -

## Slide 22: General
Cranes
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Gearbox / Reducer | ISO VG 320 or 460 FZG Temperature range | High temperature | PETRONAS Gear MEP* | PETRONAS Gear FL | PETRONAS Gear Syn PAG
Electric motors | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Bearings (Grease) | Li complex / Ca Sulfonate complex NLGI 2 380 – 460 base oil viscosity Dust handling polymer thickener | Extreme High temperature Water Extreme load carrying | PETRONAS Grease LiX EP 2/380 |  | PETRONAS Grease LiX Syn 2/220

## Slide 23: General
Dump trucks and loaders
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Engine | Engine Oil 15W40 / 10W40 | Cold starting Long idling periods Soot handling | PETRONAS Urania LD 7 ** | PETRONAS Urania 5000 E 15W40 | PETRONAS Urania 7000 E 10W40 **
Cooling System | Coolant Fluid | Long periods of work High temperature | PETRONAS Paraflu 11 ** | PETRONAS Paraflu Up Ready ** | -
Transmission | SAE 30 TO-4 series | Long drain intervals High temperature handling High load capability | PETRONAS Powertrans T4 30W ** | - | -
Converter | SAE 30 TO-4 series | Long drain intervals High temperature handling High load capability | PETRONAS Powertrans T4 30W ** | - | -
Hydraulics / Steering | SAE 10W TO-4 series | Long drain intervals High temperature handling High load capability | PETRONAS Powertrans T4 10W ** | - | -
Fire Resistant Hydraulic System | Fire resistant Premium VI High VI | Fire Resistance | PETRONAS Hydraulic HFC | PETRONAS Hydraulic FR | -
Final Drive | SAE 50 TO-4 series | Long drain intervals High temperature handling High load capability | PETRONAS Powertrans T4 50W ** | - | -
Grease points | NLGI 2 EP | With solid lubricants Water tolerance High load capability | PETRONAS Grease LiX MEP | PETRONAS Grease LiCa MG HL | PETRONAS Grease LiCa MG XHL

## Slide 24: General
Blowers
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Bearings (Grease) | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease Li EP 2 | PETRONAS Grease CaSx | PETRONAS Grease LiX Syn 2/220
Gearbox / Reducer / Bearings (Oil) | AGMA 4-7 EP | Micropitting resistance High load capability Low foaming tendencies Water separability | PETRONAS Gear MEP * | PETRONAS Gear FL | PETRONAS Gear Syn PAO
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -

## Slide 25: General
Pumps
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Bearings (Oil) | ISO VG 68 | Demulsibity Low foaming tendencies Antiwear properties | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF
Bearings (Grease) | NLGI 2 EP | High load capability Water tolerance Long life | PETRONAS Grease Li EP 2 | PETRONAS Grease CaSx | PETRONAS Grease LiX Syn 2/220
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -

## Slide 26: General
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Air compressor | 51506-VDL | Oxidation stability Good air release Foam tendencies | PETRONAS Compressor A M2 | PETRONAS Compressor A M4 | PETRONAS Compressor A Syn PAO
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Air Compressors

## Slide 27: General
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Bearings (Grease) | NLGI 2 EP | High load capability Extreme water tolerance Long life | PETRONAS Grease Li EP 2 |  | PETRONAS Grease LiX Syn 2/220
Bearings (Oil) | ISO VG range | Demulsibity Low foaming tendencies Antiwear properties | PETRONAS Jenteram | Petronas Jenteram G | PETRONAS Jenteram Syn
Diesel Engine Oil | Engine Oil 15W40 / 10W40 | Cold starting Long idling periods Soot handling | PETRONAS Urania LD 7 ** | PETRONAS Urania 5000 E 15W40 | PETRONAS Urania 7000 E 10W40 **
Cooling System | Coolant Fluid | Long periods of work High temperature | PETRONAS Paraflu 11 ** | PETRONAS Paraflu Up Ready ** | -
Electric Motor Bearings | NLGI 2 | Long life at high temperature Low bleed Medium and high speed | PETRONAS Grease Li 2 | PETRONAS Grease PU | -
Gas Turbine | ISO VG range | Demulsibity Low foaming tendencies Antiwear properties | PETRONAS Jenteram | Petronas Jenteram G | PETRONAS Jenteram Syn
Gearbox / Reducer | ISO VG range | Demulsibity Low foaming tendencies Antiwear properties | PETRONAS Jenteram | Petronas Jenteram G | PETRONAS Jenteram Syn
Back Up Generators - Diesel & Gas Turbine

## Slide 28: General
Component Part | Lube Spec | Lube Requirements | Products |  | 
 |  |  | Standard | Premium | Supreme
Cutting fluids |  | High emulsion stability Excellent lubricity and anti-weld Anti-rust, anti-corrosion Anti-sludge Anti-bacterial | Mecafluid SM 59** | Mecafluid S 2006 ** | -
Grease points | NLGI 2 EP | Water tolerance High load capability | PETRONAS Grease Li EP 2 |  | PETRONAS Grease LiX Syn 2/220
Hydraulics | ISO VG range HM specification | Good air release Water separability Low foaming tendencies | PETRONAS Hydraulic | PETRONAS Hydraulic HV | PETRONAS Hydraulic ESF
Slide way oils | ISO VG 68 and 220 Cincinnati Machine Spec | Pumpability and sprayability Adhesive characteristics Extreme pressure | PETRONAS Slideway | - | -
Machinery Workshops